L10 - 	WINDOWS

316	STEEL WINDOWS AND DOORS:

-	Manufacturer and reference: Crittall Windows Ltd, Corporate® MW40 range

-	Generally manufactured in accordance with BS 6510 MW40 section.

-	Weathertightness: To BS 6375: Part 1. Exposure category (Design wind pressure): 1200 | 2000 (Pa) see Table AA

-	For air permeability, water-tightness and wind resistance data see Table AA

-	Operation and strength characteristics:  To BS 6375: Part 2

-	Construction:  All frames have welded corners and are flat and square within normal	manufacturing dimensional tolerances of +/- 1.5 mm.  Intermediate bars are hot tenon riveted.

-	Galvanising: All components including steel attachments, coupling members and ancillaries to be hot-dipped after manufacture to BS EN ISO 1461:2009

-	Glazing details: Will accept double glazing up to 30 mm in thickness.

Glazing beads present no horizontal ledges on which dust and dirt can gather.

DG units to have a maximum centre pane U value of 1.2 W/m²/K compliant with Part L 2010 (2013 Edition)

-    	Weatherstripping: Compressible closed cell foam tape weatherseal

-	Ironmongery | accessories:  See clause 328.

-	Finish as delivered: Galvanised and Duralife® polyester powder coated in a range of colours (see clause 331).

325	STEEL WINDOWS AND DOORS:

-	Generally all the foregoing.

-	Manufacturing undertaken in the Crittall factory by directly employed personnel.

-	Design, manufacture and installation carried out under Quality Management Systems certified to BS EN ISO 9001

-	Manufacture to be undertaken under an Environmental Management System accredited to BS EN ISO 140001

328	IRONMONGERY | ACCESSORIES:

-	Standard provisions:  See Brochure/Binder

-	Standard finishes:  	Satin anodised or satin chrome according to fitting.

-	Optional hardware | finishes:  Available, consult Crittall.

331	FINISH COATING

-	Type | reference:  Epoxy free Duralife® polyester powder coating using Interpon D1036 powder to BS EN ISO 13438

-	Preparation:  Following galvanising, windows are chemically cleaned and pre-treated to provide surface to which powder coating will adhere.

-	Covering:  Minimum 60 microns on all significant surfaces.

-	Colours:    Wide selection available. See Crittall Colour Selector.

-	Process:   Coating must be undertaken in the same manufacturing plant as the frame fabrication.

470	SEALANTS

- Joint surfaces are to be clean, grease | dust free and prepared in accordance with the sealant manufacturers recommendations

- External perimeter sealant is to be Arbosil 1096 or 1090 neutral cure low modulus silicone compliant with BS 5889 Type A 1989.

552	METAL GLAZED SCREENS:

-	Screen | composite window assemblies are available utilising all Crittall ranges.

-	A full design | advice service is available.

-	Coupling details; consult Crittall.

## Table AA

| Type of Opening Light Corporate® MW40 | Exposure Category (Pa) | Air Permeability Not More Than 16m3/h/m Joint at (Pa) | Water Tightness No Leakage at (Pa) | Wind Resistance No Damage & Only Permissible Deflection at (Pa) |
| --- | --- | --- | --- | --- |
| Vertical Pivot | 1200 | 300 | 50 | *1200 |
| Horizontal Pivot | 1200 | 300 | 100 | *1200 |
| Bottom Hung Open In | 1200 | 300 | 100 | *1200 |
| Side Hung Open In | 1200 | 300 | 100 | *1200 |
| Side Hung Open Out | 2000 | 300 | 300 | 2000 |
| Top Hung Open Out | 2000 | 300 | 300 | 2000 |
| Single Door Open Out ** | 800x | 150 | 50 | 800 |
| Double Door Open Out ** | 800x | 150 | 50 | 800 |

* 	A higher wind resistance can be achieved

**	Applies to doors with a full rebated threshold. Thresholds designed to meet accessibility requirements of the UK Building Regulations are unlikely to meet category 800x

∆	Windows fitted with manual or electrically operated winding gear may not achieve the performance detailed in Table AA