L10	WINDOWS

320	STEEL WINDOWS:

-	Manufacturer and reference:  Crittall Windows Limited, Homelight® Plus Residential.

-	Windows generally manufactured in accordance with BS 6510

-	Weathertightness: To BS 6375: Part 1. Exposure category (design wind pressure):   2000 (Pa).

-	For air permeability, water-tightness and wind resistance data see Table AA

-	Operation and strength characteristics: To BS 6375: Part 2.

-	Construction: All frames have welded corners and are flat and square within normal manufacturing dimensional tolerances of ± 1.5mm.

-	Galvanising: All components including steel attachments, coupling members and ancillaries to be hot dipped after manufactured to BS EN ISO 1461:1999.

-	Glazing details: 16 mm DG units comprising:

DG units to have a maximum centre pane U value of 1.2 W/m²/K compliant with Building Regulation Part L 2010

Sloping glazing beads present no horizontal ledges on which dust and dirt can gather.

-	Weatherstripping: Pressure equalised and fitted with twin gaskets	(external rainscreen/internal air seal) in a co-extrusion with hot melted adhesive applied.

-	Ironmongery/accessories: Clause 328.

-	Finish as delivered: Galvanised and Duralife® polyester powder coated (see clause 331).

325	STEEL WINDOWS:

-	Manufacturing undertaken in a factory sited in the UK and within 100 mile radius of the site to minimise the carbon footprint of the window renewal programme.

-	Design, manufacture and installation carried out under a Quality Management System certified to BS EN ISO 9001

-	Manufacture to be undertaken under an Environmental Management System accredited to BS EN ISO 14001.

328	IRONMONGERY/ACCESSORIES:

-	Standard provisions:  See Brochure/Binder

-	Standard finishes:        Satin anodised or satin chrome according to fitting.

-	        Optional hardware | finishes:  Available, consult Crittall.

331	FINISH COATING

-	Type/reference: Epoxy free Duralife® polyester powder coating using Interpon D36 powder to BS EN ISO 13438.

-	Preparation: Following galvanising, windows are chemically cleaned and pre-treated to provide surface to which powder coating will adhere.

-	Covering:  Minimum 60 microns on all significant surfaces.

-	Colours:    Wide selection available. See Crittall Colour Selector.

-	Process:  Coating must be undertaken in the same manufacturing plant as the frame fabrication.

810	SEALANT JOINTS

- External perimeter sealant to be Adshead Ratcliffe Arbosil 1096 or 1090 low modulus neutral cure silicone sealant to BS5889 Type A: 1999

812	COMPOSITE TIMBER | EXTRUDED ALUMINIUM SUBFRAMES

- Subframes to be constructed from a primed engineered soft wood main frame profiled to match the existing subframe with Duralife® polyester powder coated aluminium extrusions applied externally to match the original timber profiles

- Subframes to be factory assembled

- Timber to be factory finished with 1 coat of Teknos Aquaprimer 2901 + 1 coat Teknos Aquatop 2600 coloured RAL 9911 satin

Table AA

| TYPE OF OPENING LIGHT Homelight® Plus | EXPOSURE CATEGORY (Pa) | AIR PERMEABILITY: Not More Than 16m3/h/m JOINT, AT (Pa) | WATER TIGHTNESS: NO LEAKAGE, AT (Pa) | WIND RESISTANCE: NO DAMAGE & ONLY PERMISSABLE DEFLECTION, AT (Pa) |
| --- | --- | --- | --- | --- |
| Side Hung Open Out | 2000 | 300 | 200 | 2000 |
| Top Hung Open Out | 2000 | 300 | 200 | 2000 |