L10 - 	WINDOWS

316	STEEL WINDOWS AND DOORS:

-	Manufacturer and reference: Crittall Windows Ltd, Innervision® range

-	Generally manufactured in accordance with BS 6510, W20 section

-	Operation and strength characteristics:  To BS 6375: Part 2

-	Construction:  All frames have welded corners and are flat and square within normal	manufacturing dimensional tolerances of +/- 1.5 mm.  Intermediate bars are hot tenon riveted

-	Galvanizing:  All components including steel attachments, coupling members and ancillaries:  hot-dipped after manufacture to BS EN ISO 1461

-	Glazing details:  Will accept single or double glazing up to 16.4 mm in thickness

Glazing beads present no horizontal ledges on which dust and dirt can gather

-    	Draughtproofing: Gaskets complying with BS 4255: Part 1, manufactured from EPDM,	secured into grooves of opening frame with adhesive

Sliding doors include woven pile draught strips secured into jamb extrusions, and applied EPDM compressible seals

-	Ironmongery/accessories:  See clause 328

-	Finish as delivered:  Galvanized and Duralife™ polyester powder coated (see clause 331) in a 	range of colours

325	STEEL WINDOWS AND DOORS:

- Generally, all the foregoing

- Manufacturing undertaken in the Crittall factory by directly employed personnel

- Design, manufacture, and installation carried out under Quality Management Systems certified to BS EN ISO 9001

- Manufacturing undertaken under an Environmental Management System certified to BS EN ISO 140001

328	IRONMONGERY/ACCESSORIES:

-	Standard provisions:  See Brochure

-	Standard finishes:  RTD (Bronze Effect) or Satin Chrome

-	Optional hardware/finishes:  Available, consult Crittall

331	FINISH COATING:

-	Type/reference:  Epoxy free Duralife® polyester powder coating using Interpon D36 powder

-	To BS EN ISO 13438

-	Preparation:  Following galvanizing, windows are chemically cleaned and pre-treated to provide a surface to which powder coating will adhere

-	Covering:  Minimum 60 microns on all significant surfaces

-	Colours:  Wide selection available.  See Crittall Duralife® Standard Colour Guide

-	Process:  Coating will be undertaken in the same manufacturing plant as the frame fabrication

470	SEALANT:

- Joint surfaces are to be clean, grease / dust free and prepared in accordance with the sealant manufacturer’s recommendations

- Glazing top-capping, perimeter sealant and coupling sealant is to be a neutral cure, low modulus silicone compliant with BS 5889 Type A 1989

552	METAL GLAZED SCREENS:

-	Screens/coupled assemblies are available, utilising all Crittall ranges

-	A full design/advice service is available

-	Coupling details; consult Crittall