L10 - 	WINDOWS

316	STEEL WINDOWS AND DOORS:

-	Manufacturer and reference: Crittall Windows Ltd, Corporate® MW40 range

-	Manufactured generally in accordance with BS 6510, MW40 section

-	Weathertightness: To BS 6375 Part 1

Exposure category (Design Wind Pressure): 1200 / 2000 (Pa)

-	For air permeability, watertightness and wind resistance data see Table AA

-	Operation and strength characteristics:  To BS 6375 Part 2

-	Construction:  All frames have welded corners and are flat and square within normal	manufacturing dimensional tolerances of +/- 1.5mm.  Intermediate bars are hot tenon riveted

-	Galvanising: All components including steel attachments, coupling members and ancillaries are hot-dipped after manufacture to BS EN ISO 1461

-	Glazing details: Will accept double glazing up to 30.8mm in thickness

Glazing beads present no horizontal ledges on which dust and dirt can gather

-    	Weatherstripping: Compressible closed cell foam tape weatherseal

-	Ironmongery / accessories:  See clause 328

-	Finish as delivered:  Galvanized and Duralife™ polyester powder coating (see clause 331) in a range of colours

325	STEEL WINDOWS AND DOORS:

-	Generally, all the foregoing

-	Manufacturing undertaken in the Crittall factory by directly employed personnel

-	Design, manufacture and installation carried out under Quality Management Systems certified to BS EN ISO 9001

-	Manufacture to be undertaken under an Environmental Management System certified to BS EN ISO 140001

328	IRONMONGERY / ACCESSORIES:

-	Standard provisions:  See Brochure

-	Standard finishes:  RTD (Bronze Effect) or Satin Chrome

-	Optional hardware/finishes:  Available, consult Crittall

331	FINISH COATING

-	Type/reference:  Epoxy free Duralife® polyester powder coating using Interpon D36 powder

-	To BS EN ISO 13438

-	Preparation:  Following galvanizing, windows are chemically cleaned and pre-treated to provide a surface to which powder coating will adhere

-	Covering:  Minimum 60 microns on all significant surfaces

-	Colours:  Wide selection available.  See Crittall Duralife® Standard Colour Guide

-	Process:  Coating will be undertaken in the same manufacturing plant as the frame fabrication

470	SEALANT:

- Joint surfaces are to be clean, grease / dust free and prepared in accordance with the sealant manufacturer’s recommendations

- Glazing top-capping, perimeter sealant and coupling sealant is to be a neutral cure, low modulus silicone compliant with BS 5889 Type A 1989

552	METAL GLAZED SCREENS:

- Screens/coupled assemblies are available, utilising all Crittall ranges

- A full design/advice service is available

- Coupling details: consult Crittall

## Table AA

| TYPE OF CORPORATE® MW40 WINDOW OR DOOR | EXPOSURE CATEGORY (Pa) | AIR PERMEABILITY: Not More Than 16m3/hr/m JOINT, AT (Pa) | WATER-TIGHTNESS: NO LEAKAGE, AT (Pa) | WIND RESISTANCE: NO DAMAGE & ONLY PERMISSABLE DEFLECTION, AT (Pa) |
| --- | --- | --- | --- | --- |
| Side Hung Open Out | 2000 | 300 | 300 | 2000 |
| Side Hung Open In | 1200 | 300 | 100 | 1200 |
| Folding Window Open Out | 2000 | 300 | 300 | 2000 |
| Folding Window Open In | 1200 | 300 | 100 | 1200 |
| Projecting Side Hung Open Out | 2000 | 300 | 300 | 2000 |
| Projecting Side Hung Open In | 1200 | 300 | 100 | 1200 |
| Top Hung Open Out | 2000 | 300 | 300 | 2000 |
| Projecting Top Hung Open Out | 2000 | 300 | 300 | 2000 |
| Bottom Hung Open In | 1200 | 300 | 100 | 1200 |
| Vertical Pivot | 1200 | 300 | 50 | 1200 |
| Horizontal Pivot | 1200 | 300 | 100 | 1200 |
| Door – open out rebated outer frame | 1200 | 300 | 100 | 1200 |
| Door – open in rebated outer frame | 1200 | 300 | 100 | 1200 |
| Notes: - Windows fitted with remote operating gear (electric or manual) may not achieve the performance listed - Door performance relates to both single and double doors - Should greater project weather performance be required, please refer to Crittall Technical for advice |  |  |  |  |