[image: image1.jpg]


CRITTALL WINDOWS NBS SPECIFICATION

T60® RANGE


L10 - 
WINDOWS
316 STEEL WINDOWS AND DOORS:
· Manufacturer and reference: Crittall Windows Ltd, T60® Thermal Break
· Manufactured generally in accordance with BS 6510
· Operation and strength characteristics:  To BS 6375: Part 2 and BS EN 14024
· Weathertightness:  To BS 6375: Part 1
· Exposure Category (Design Wind Pressure):  Up to 2000 (Pa)
· For air permeability, watertightness and wind resistance data see Table AA

· Construction

· All frames have welded corners and are flat and square within normal manufacturing tolerances of +/-1.5 mm

· Thermally broken profiles tested in accordance with EN 14024 with density of 1.8 kg/dm3, tensile strength of 600 MPa and E-modulus of 25000 MPa
· Thermal break:  Profiles feature integral polyurethane GRP thermal isolators (67% fibreglass content)
· Product range: Fixed lights (single section), top hung, projecting top hung, side hung, bottom hung and french casement open in and open out, internally glazed configurations available.
· Sightlines for T60® profiles:

· Fixed frames:  25mm / 40mm

· Operable windows:  45mm / 60mm

· Glazing bars:  True, 40mm. Simulated divided light grids available from 19mm

· Glazing details

· Will accept insulating glass units up to 36mm in thickness

· Frames are delivered unglazed for site glazing - Crittall will supply frames only, or frames with glazing units

· The thickness of glazing units will determine the types of gaskets and beads supplied

· Wet glazing or gasket glazing options available, depending on application

· Glazing beads

· Clip-in polyester powder coated (as frame colour) aluminium glazing beads

· Fixed to frames using purpose-made glazing clips

· Available in 3 depths to suit varying glass thicknesses
· Weatherstripping: EPDM gaskets secured into grooves of opening frames
· Ironmongery/accessories:  See clause 328
· Corrosion protection:  See clause 331
· Finish as delivered:  See clause 331
325
STEEL WINDOWS AND DOORS:
· Generally, all the foregoing

· Manufacturing undertaken in the Crittall factory by directly employed personnel

· Design, manufacture, and installation carried out under Quality Management Systems certified to BS EN ISO 9001

· Manufacture is undertaken under an Environmental Management System certified to BS EN ISO 140001

328
IRONMONGERY/ACCESSORIES

· Standard provisions:  Refer to brochure

· Standard finishes:  RTD (Bronze Effect) or Satin Chrome

· Optional hardware/finishes:  Available, including multi-point locking option. Consult Crittall

331
FINISH COATING

· Type/reference:  Epoxy free Duralife™ polyester powder coating to BS EN 13438, primed with Interpon ALZ90F zinc-rich powder and top-coated with Interpon D1036 or D2525 powder applied in accordance with BS EN ISO 13438
· Substrate:  Thermally broken steel, with protection coating of type ZF100 (Galvannealed Zinc-Iron) at @100 g/m2 (approximately 6 µm)
· Preparation:  Chemical clean and pre-treat the ZF100 coated substrate to provide a surface to which zinc primer and powder coating will adhere

· Covering:  Minimum 60 micrometres per coat on all significant surfaces
· Colours:  Wide selection available.  See Crittall Duralife™ Standard Colour Guide
· Process:  

· Coating will be undertaken in the same manufacturing plant as the frame fabrication

· Applied in accordance with quality control inspection measures conforming to ISO 9001

470
SEALANT:
· Joint surfaces are to be clean, grease / dust free and prepared in accordance with the sealant manufacturer’s recommendations

· Glazing top-capping, perimeter sealant and coupling sealant is to be a neutral cure, low modulus silicone compliant with BS 5889 Type A 1989

552
METAL GLAZED SCREENS

· Multilights / direct-coupled assemblies are available

· A full design / advice service is available

Table AA

	Type of T60® Window or Door
	Frame Size Performance Split-Limits*
	Air Permeability

to BS EN 12207
	Watertightness

to BS EN 12208
	Wind Resistance

to BS EN 12210

	
	
	Class (Pa)

	
	
	
	

	Fixed Light (single section)
	4 (600)
	E1200
	C5/B5 (2000)

	Side Hung open-out
	≤810 x 1610mm H
	4 (600)
	E900
	C5/B5 (2000)

	
	≤810 x 2210mm H
	4 (600)
	E900
	C4/B4 (1600)

	
	≤1010 x 2410mm H
	3 (600)
	E750
	C4/B4 (1600)

	Side Hung open-in
	≤810 x 1610mm H
	4 (600)
	E900
	C5/B5 (2000)

	
	≤810 x 2210mm H
	4 (600)
	E900
	C4/B4 (1600)

	
	≤1010 x 2410mm H
	3 (600)
	7A (300)
	C4/B4 (1600)

	French Casement
open-out
	≤840 x 1610mm H
	4 (600)
	9A (600)
	C3/B3 (1200)

	
	≤840 x 2210mm H
	4 (600)
	8A (450)
	C3/B3 (1200)

	
	≤1990 x 2410mm H
	3 (600)
	8A (450)
	C3/B3 (1200)

	French Casement

open-in
	≤840 x 1610mm H
	4 (600)
	9A (600)
	C3/B3 (1200)

	
	≤840 x 2210mm H
	4 (600)
	8A (450)
	C3/B3 (1200)

	
	≤1990 x 2410mm H
	3 (600)
	8A (450)
	C3/B3 (1200)

	Bottom Hung open-in
	≤2210 x 810mm H
	4 (600)
	E750
	C4/B4 (1600)

	
	≤2410 x 1010mm H
	3 (600)
	7A (300)
	C4/B4 (1600)

	Top Hung open-out
	≤1660 x 690mm H
	4 (600)
	9A (600)
	C3/B3 (1200)

	Projecting Top Hung
open-out
	≤1200 x 1450mm H


	4 (600)
	9A (600)
	C4/B4 (1600)

	Single Leaf Door open-out
	≤1010 x 2310mm H
	2 (300)
	8A (450)
	C4/B4/A4 (1600)

	
	≤1010 x 2510mm H
	4 (600)
	8A (450)
	C4/B4/A4 (1600)

	Single Leaf Door open-in
	≤1010 x 2310mm H
	4 (600)
	6A (250)
	C4/B4/A4 (1600)

	
	≤1010 x 2510mm H
	4 (600)
	6A (250)
	C4/B4/A4 (1600)

	Double Leaf Door open-out
	≤1990 x 2310mm H
	3 (600)
	8A (450)
	C3/B3/A4 (1200)

	
	≤1990 x 2510mm H
	3 (600)
	6A (250)
	C3/B3/A4 (1200)

	Double Leaf Door open-in
	≤1990 x 2310mm H
	3 (600)
	4A (150)
	C3/B3/A4 (1200)

	
	≤1990 x 2510mm H
	3 (600)
	4A (150)
	C3/B3/A4 (1200)

	Notes

1. Windows fitted with remote operating gear (electric or manual) may not achieve the performance listed

2. *Sizes are overall web, outer frame(s)

3. Performance figures for windows vary depending on hardware selection. Maximum shown

4. Performance figures for doors vary depending on threshold selection. Maximum shown


Revision Date 29 April 2025
Crittall Windows Limited Francis House Freebournes Road Witham Essex CM8 3UN Tel: 01376 530800

email: hq@crittall-windows.co.uk  website: http://www.crittall-windows.co.uk

